## Slide 1: Sulfur Isotopes in Sulfides using Secondary Ion Mass Spectrometry (SIMS)
Glenn Piercey
SIMS Lab - CREAIT

## Slide 2
Sample Preparation
SIMS Instrument
Data Analysis
Case Studies
- Lemarchant Deposit – Central NL
- Ming Deposit – Central NL
- Voisey’s Bay – Northern Labrador
Sulfur Isotopes in Sulfides using SIMS

## Slide 3
Sample Preparation
Drill Rig
Drill Core
Selecting
Sectioning/
epoxy/
polishing
Sample gold
coating

## Slide 4
Sample Preparation: Mapping
SIMS Sulfide Puck
4x Image Galena
10x Image Galena

## Slide 6
Two sources used to produce primary ions:
1. Duoplasmatron (DP)- uses oxygen to
produce O- or O2+ ions.
2. Cesium Ionization Source – produces Cs+
ions.
Ions extracted from sources pass through a
primary beam mass filter (PBMF) to remove
unwanted species from beam.
Electrostatic lenses and apertures control
the intensity and size of the primary beam
hitting the sample.
Primary Column

## Slide 8: Mass Spectrometer
Electrostatic Analyzer (ESA) and Magnet work to separate secondary ions by mass, charge and energy resulting in only ions of interest hitting the detection/counting system.

## Slide 9
Video Tour of SIMS Lab (5 minutes) 500MB video

## Slide 10: Sample Analysis: Sulfur Stable Isotopes
34S/32S = ratio of heavy isotope to light
δ34S = ‰ ( per mil)
= difference in isotope
composition of sample relative to
international standard, VCDT.
δ34S = R sample – R standard/ Rstandard x 1000

## Slide 11: Sample Analysis: Standard Development
SIMS, Solution ICP-MS, Laser ICP-MS, IRMS
Matrix match, homogenous
Chalcopyrite = Norilsk (8.4 ‰ VCDT)
Pyrrhotite = PoW1 (3.0 ‰ VCDT)
= TrW1 (-2.6 ‰ VCDT)
Pyrite = UL9 (16.3 ‰ VCDT)
= KH87 (0.4 ‰ VCDT)
Galena = HT10 (14.6 ‰ VCDT)
Arsenopyrite = (ARSPY57 3.1‰ VCDT)

## Slide 12
Sulfur (S) Isotope Geochemistry
Information gained from variations in isotopic 34S/32S composition of sulfide minerals
Variation caused by temperature and oxidation and reduction reactions on S.

## Slide 13
Main Sulfur Sources in an Ore Deposit:
Sulfide minerals such as pyrite (FeS2), galena (PbS), and chalcopyrite (CuFeS2) are formed by binding metal with sulfide.
Sulfur sources within these sulfides are:
Magmatic sources– fractionation restricted (0+/-3per mil)
Thermochemical sulfate reduction (TSR) of seawater sulfate
Bacterial sulfate reduction (BSR) – anaerobic bacteria reducing seawater sulfate
Igneous, metamorphic and/or sedimentary wall rock.

## Slide 14
CASE STUDY 1:
Multiple Sulphur and lead sources recorded in hydrothermal exhalites associated with the Lemarchant volcanogenic massive sulfide (VMS) deposit, central Newfoundland, Canada
Lode, Piercey, Layne, Piercey and Cloutier, 2017. Mineralium Deposita 52: 105-128.
d34S systematics indicate sulfur predominantly biogenically derived from Baterial sulfate reduction (BSR) of seawater sulfate.
Some sulfides near vent contain a higher proportional of sulfur from thermochemical sulfate reduction (TSR).

## Slide 15
Thermochemical S source for sulfides
Biogenic S source for sulfides

## Slide 16
CASE STUDY 2:
Variations of sulphur isotope signatures in sulphides from the metamorphosed Ming Cu(−Au) volcanogenic massive sulphide (VMS) deposit, Newfoundland Appalachians, Canada
Brueckner, Piercey, Layne, Piercey & Sylvester (2014) 50(5): 619-640
Sources of Sulfur at Ming VMS Deposit:
Thermochemical sulfate reduction (TSR)
-Silicified horizon consistent with sulfur from TSR.
Sulfur leached from igneous wall of magmatic fluids
- Mixing of reduced seawater sulfate with igneous sulfur.
- The influence of igneous sulfur increases with temperature.

## Slide 18
S Sources in Magmatic Ni-Cu (Voisey’s Bay):
• The Tasiuyak Gneiss (country rock) more deplete S signature range (produced by BSR= -2 to -17‰).
• Enderbitic gneiss (country rock), S signature around 0‰
• Mantle derived sulfur (0 +/- 3‰)
CASE STUDY 3:
Sulfur and oxygen isotopic evidence of country rock contamination
in the Voisey’s Bay Ni-Cu-Co deposit, Labrador, Canada
Ripley, Park, Li and Naldrett (1999) Lithos 47: 53-68

## Slide 20
Reid Brook = 50% S from country rock
Eastern Deeps N Troctolite = Mantle Derived S
Eastern Deeps, Discovery Hill, Ovoid = mixing between mantle and country rock